Polycarboxylate superplasticizer cas no.24936-68-3

Introduction

Polycarboxylate Superplasticizer with cas no.24936-68-3 is used as a high range water reducing admixture in high performance concrete, high strength concrete, high volume fly ash/slag concrete, cement grouting, and dry mortar. These polymers are used as dispersants, especially for early strength concrete, to avoid particle segregation. They have good water reducing even with low dosage and have excellent durability.

Advantages/Characteristics:

- Improve the durability and impermeability of concrete and reduce the contractibility, efficiently reduce the bad effects of crack of concrete.

2.Excellent compatibility with various types of cements.

3.Low blend dosage and high water reduction

4.Greatly improve the early and late strength of concrete.

5.Low chloride and alkali content, no corrosion to steel-bar.

6.Green environmental protection, pollution-free, formaldehyde-free other pollution elements.

Production methods

It was synthesized from unsaturated acid as monomer by free radical polymerization in the presence of initiator.

Use

Use of polycarboxylic acid: used for cooling water circulation, oilfield water injection and other scale dispersant.

Application:

- Suits for different types of cement and acts as good dispersant, especially for early strength cement.

Quality Specification

| Items | Specification |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SPC-02 Liquid(water reducing type) | SPS-03 Liquid(slump retention type) | SPS-04 Liquid (Early strength & water reducing type) | SPS-05 Liquid(long slump retention type) | SPS-06 powder(Water reducing type | SPS-08 Powder(Water reducing type) |
| Appearance | White or light yellow to brown viscous liquid | White or light yellow to brown viscous liquid | Colorless or light yellow to brown viscous liquid | Colorless to light yellow viscous liquid | White or light yellow powder | White powder |
| Density | 1.10±0.02 g/cm³ | 1.10±0.02 g/cm³ | / | 1.10±0.02 g/cm³ | 500±50 Kg/m³ | 500±50 Kg/m³ |
| pH (23℃) | 5--7 | 5--7 | 6±1 | 5--7 | 6.0±1.0 | 6.0±1.0 |
| Solid Content% | 50±1.0 | 50±1.0 | 50±1 | 50±1.0 | 97.0±1.0 | 97.0±1.0 |
| Moisture content% | / | / | / | / | ≤3.0 | ≤3.0 |
| Water Reducing Ratio% | / | ≥15 | ≥25 | ≥ 15 | ≥25 | ≥25 |
| Cl- % | ≤0.02 | ≤0.02 | ≤0.02 | ≤0.02 | ≤0.02 | ≤0.02 |
| Alkali content% | ≤0.3 | ≤0.3 | ≤0.3 | / | ≤0.3 | ≤0.3 |
| Na2SO4 % | / | / | / | ≤0.3 | / | / |

Package: Packed in 25kg plastic woven bags with PE inner liner, 16 mt with pallets loaded in one 20’GP, 27 mt with pallets loaded in 40’HQ by sea, 25.5 mt with pallets loaded in 40’HQ by train

Contact information:

Shelly Cui

Ella Yang

The seller: Zibo Zhuoxing Enterprises Co., Ltd.

Add: Room 1103, 11th Floor, Yunlong Plaza B, No.28 Huaguang Road, Zhangdian District, Zibo City，Shandong Province, China 255000

Manufacturer: Shandong Zhuoxing Chemical Co., Ltd.

Add: Xinhai Industrial Zone, Wudi County, Binzhou City, Shandong Province, China

Tel/Fax:0086 533 2284032

Mobile/ Wechat:0086 13053363281, 0086 18615126163,

0086 17865273019

Mail:sales@zhuoxingchem.com     shellypce@hotmail.com

sales02@zhuoxingchem.com

Web site:www.zhuoxingchem.com

http://sdzhuoxing.en.alibaba.com

https://www.sdzhuoxingpce.com